Equipment

| Name | Supplier |
| --- | --- |
| Acetone | IC |
| Cotton Buds | RAL |
| Melinex tape | RAL |
| Paintbrush | RAL |
| Mixing pot | RAL |
| Mixing Spatula | RAL |
| Gloves | IC |
| Wipes | IC |
| CPR600 Resin | RAL |
| ANC506 Hardener | RAL |
| Spreader | RAL |
| Dispensing gun | IC |
| Dispensing gun nozzle | IC |
| CPR600 Resin (with carbon black pigment) | RAL |

Material Safety Data Sheets

| CPR600 (SER 300) | Pdf Attached |
| --- | --- |
| Araldite 2011 | Pdf Attached |
| ANC506 Hardener | Pdf Attached |

Method

- Glue scintillating fibre (or clear fibre) to frames (or connector) - Location – IC

  - Clean frames with acetone.

  - Place release film on jig.

  - Fix frames (or connector) to jig and wind fibres.

  - Place melinex tape over fibres to hold them still.

  - Mix 2/3 CPR600 and 1/3 ANC506 in a mixing pot (Required: spatula, gloves, wipes, extraction).

  - Apply resin mixture to fibres using paintbrush.

  - Room cure for 24 hours (or heat to 40-50° to speed up cure).

  - Repeat on underside of jig.

- Apply araldite - Location – IC

  - Once resin is cured use araldite 2011 cartridge with dispensing gun and nozzle.

  - Build up layers of araldite to help with polishing stages.

- Potting – Location - RAL

  - Transport assembled stations to RAL.

  - Pott frames using CPR600.

Note: Need to check light proofing requirements of room.